# PRODUCT DATA SHEET

# DECORATIVE CONCRETE SEALER

# Thermoplastic Acrylic Resin Solution for Concrete Surfaces

Issue Date: May 2019

# Description:

South Coast Decorative Concrete Sealer is an acrylic copolymer solution used for paint-sealing concrete and cement masonry surfaces. The product normally exhibits excellent gloss retention, colour uniformity and chalk resistance and may be approved, under certain conditions, as a concrete curing aid for cast-in-place decorative concrete flatwork.

# Performance:

# Excellent weather resistance – UV Stabilised

# Excellent alkali resistance

# Excellent colour uniformity over various porosity surfaces

# High degree of general chemical resistance and toughness

# Excellent overall properties of durability, appearance and general protection

# SPECIFICATIONS:

Characteristics								Specification

Appearance								Clear and clean

Colour (Gardner)								Less than 1

Viscosity (B4 cup, @ 25°C)						35 – 45 sec.

Solid Content, % (150°C X 30mins)						25±1

Density (@25°C)								0.92 – 0.93

Acid Value (mg KOH/g, solid)						2 – 6

Solvent								               Xylene

# TYPICAL PERFORMANCE DATA:

Pigment / Binder								1.4/1

Film Thickness (wet)							4 mils

(Page 1 of 2)

__________________________________________________________________________________

# Gloss (60°)

Glass Plate								53 up

Cementitious board							75 up

Tack Free (30°C)								14 – 16 mins

Alkali resistance (5% NaOH, one week)				Gloss retention, no blister

Water resistance								Excellent

Anti-sagging (vertical brush for cementitious board)				Pass

Weather resistance test (ASTM G-53-77)					168 hrs

# Test cycle: 4hrs UV at 60°C / 4hrs cond. at 40°C

Gloss retention, % (cementitious board)					98 – 100

Surface change (cementitious board)					No change

# Important PDS Information:

This information relates only to the specific material designated and may not be valid for such material used in combination with any other materials or in any process. Such information is, to the best of our knowledge and belief, accurate and reliable as of the date compiled. However no representation, warranty or guarantee is or can be made as to its accuracy reliability or completeness. It is the user’s responsibility to satisfy themselves as to the suitability and completeness of such information for their own particular use. South Coast Decorative Concrete Supplies Pty Ltd nor neither its manufacturer for its use accept any liability whatsoever of any loss or damage that may occur from use of this information, and no warranty is or can be offered against patent infringement.

South Coast Decorative Concrete Supplies Pty Ltd products are sold based on the product specifications supplied by the manufacturer listed above unless otherwise agreed by the manufacturer in writing. No representation, warranty, (expressed or implied, of [*satisfactory quality], merchantability, fitness or otherwise), or guarantee is made as to the suitability or fitness for use of the product in the customer’s specific application. It is the user’s responsibility to confirm the suitability and fitness for use of the product. Specifications are pursuant to the manufacturer’s sampling and testing procedures in effect at the time of production. Analysis may be performed on representative samples and not the actual product shipped.

# South Coast Decorative Concrete Supplies PTY Ltd

# 1 McIntyre Way Bomaderry , NSW, 2541

# Ph: 61 2 44235111 - Fax: 61 2 44235105

Web: www.scdcs.com.au

(Page 2 of 2)